MINISTRY OF DEFENCE

| DEFENCE STANDARD | NORMDEF 0004-1 |
| --- | --- |
|  | Edition 01 |
|  | JULY 2014 |

ICS:: 95.020

FRENCH TITLE: Systèmes de peinture destinés à la protection extérieure des cellules d’aéronefs militaires

Partie n° 1 : 	Exigences de performances des systèmes de peinture destinés à la protection extérieure des cellules d’aéronefs militaires

ENGLISH TITLE: Paint systems for the exterior protection of military aircraft airframes

Part n° 1: 	Performance requirements of paint systems for the exterior protection of military aircraft airframes.

ANALYSIS:

This document defines the general requirements for the protection of the exterior surfaces of military aircraft airframes by means of paint systems.

It describes the quality control principles and requirements of the paint systems. To this end, it lays down the processes to be followed for their qualification or certification.

KEY WORDS:

Paint systems – Military aircraft –Airframe –Colour – Pigments – Shade card – Shade – Definition file – Qualification – Certification

| DEFENCE STANDARD | NORMDEF 0004-1 |
| --- | --- |
|  | Edition 01 |
|  | JULY 2014 |

MODIFICATIONS:

| Edition | Date | Nature of the change |
| --- | --- | --- |
| 01 | 07.2014 | First issue. |

DOCUMENTS RENDERED OBSOLETE BY THE PRESENT ISSUE:

| Reference | Date | Subject |
| --- | --- | --- |

WRITTEN BY:

| Author: | “Materials, Components, Management of environmental risks” division (MCM) |
| --- | --- |

MAINTAINED BY:

| Maintenance: | Joint Forces Paint and Varnish Standardisation Committee (CIN-PV) |
| --- | --- |

APPROVAL AUTHORITIES:

| Approval | Chairman of the CIN-PV |
| --- | --- |
|  | Standardisation Sector Manager - Materials, Workshops and Design Offices (RSN MAB) |
|  | Director of the Defence Standardisation Centre (CND/D) |

Centre de Normalisation de Défense - Defence Standardisation Centre 16 bis, Avenue Prieur de la Côte d’Or – CS 40300 94114 ARCUEIL Cedex  : +33/0 1 79 86 36 02 -  : +33/0 1 79 86 43 63

MEMBERS of the JOINT FORCES PAINT AND VARNISH STANDARDISATION COMMITTEE  (CIN-PV):

Chairman: 	Jean-Pierre PAUTASSO	DGA/DT/ST/IP/MCM/PMA

Secretariat:	Laurent SAUQUES	DGA / DT/ST/IP/MCM/PMA

ORGANIZATIONS EXTERNAL TO THE FRENCH  MINISTRY OF DEFENCE:

Olivier BICART-SEE				DASSAULT AVIATION

Philippe BRUNET				SIPEV

Gilles CHOLVY 				NEXTER

Jean-Marc CLAVIER				MBDA

Frédéric DUHAMEL				THALES

Christian FAVENNEC 				DCNS

Annick GALPIN				AFNOR

Alain PINON 					ACQPA

Rémy REYNET				AIRBUS HELICOPTERS

INTERNAL ORGANIZATIONS OF THE FRENCH MINISTRY OF DEFENCE:

Didier BARREAU				DGA TA/MT

Pascal CHIVÉ					DGA/DT/ST/IP/MCM/PMA

Jean DESSAPT					AA/SIAé/AIA-CF

Marie - Ange DUCROS			DGA TA/EMS

Gregory EYGLUNENT				DGA MNRBC/ESD

Frédéric GUEGUEN				DCSSF/SDT/CMES/AN

Benoit HOSDEZ 				DGA / DT/ST/IP/MCM/PMA

Cédric HUBERT				DGA TA/MT

Jean-Luc LAQUA				CND

Anthony MARTIN				DGA TA/MT

Lionel MORVAN				DGA TN

Nicole NAHON				CND

Thierry POBEL					 DGA/DT/ST/IP/MCM/PMA

Philippe RICHARD				AA/SIAé/AIA-CP

Marie - Christine SAINTE CATHERINE	DGA / DT/ST/IP/MCM/PMA

Laurent SAUQUES				DGA / DT/ST/IP/MCM/PMA

Eric STIEE					DGA DT/ST/IP/CGN/OP

Mathieu VAUBOURG				SIMMT/ADCO/DP/PPB

MEMBERS OF THE WORKING GROUP SET UP BY CIN/PV:

Chairman: 	Didier BARREAU	DGA Techniques aéronautiques

Secretariat:	Didier BARREAU	DGA Techniques aéronautiques

Members:

Marie-Ange DUCROS		DGA Techniques aéronautiques

Olivier BICART-SEE	Dassault Aviation

Pierre MICHELIN		Dassault Aviation

Jean-Marc CLAVIER		MBDA-systems

Jean DESSAPT		EMAA/DCSIAé/AIA Clt-Ferrand

Frédéric DUHAMEL		THALES

Jean-Pierre PAUTASSO		DGA/DT/ST/IP/MCM/PMA

Rémy REYNET		AIRBUS HELICOPTERS

Philippe RICHARD		EMAA/DCSIAé/AIA Cuers-Pierrefeu

Maurice SARFATI		DGA/DT/ST/IP/MCM/PMA

FOREWORD

The senior command of each of the armed forces attaches considerable importance to problems relating to paint systems with regard to the operation and maintenance of military equipment. This is because some of the problems encountered during service can seriously impact flight safety, contribute to significant reductions in equipment durability or necessitate major and costly repairs.

The protective paint systems used for military aircraft must satisfy various requirements defined in the qualification programme, These requirements, in compliance with the AIR 0011 standard, in the edition dated 02/04/1996, provide the basis for the evaluation and “approval of fitness for purpose” (RAE) of the paint systems. All tests are conducted in the laboratories of the DGA.

In 2006, the DGA Aviation Programmes Department (now known as “UM AMS”), launched a comprehensive revision of the existing documents for paint systems qualification.

The present standard has been drawn up in agreement with CND and CIN PV.

This standard serves as a contractual document for the selection of paint systems for aircraft programmes.

CONTENTS

1.	OBJECT	7

2.	SCOPE	7

2.1	Types of aircraft	7

2.2	Types of environment	7

2.3	Types of application	8

2.4	Type of product	8

2.5	Nature of the substrates and type of surface preparation	8

3.	NORMATIVE REFERENCES	9

4.	TerminologY AND abBREViations	13

4.1	Terminology	13

4.2	Abbreviations	13

5.	Prerequirements for qualification	14

5.1	Documentation requirements:	14

5.2	Requirements of the paint products	14

5.2.1	Type of product	14

5.2.2	Durability	15

5.2.3	Regulatory constraints (environment, health and safety)	15

5.2.4	General requirements	15

5.2.5	Constitution of the paint system applied to exterior surfaces	15

5.2.6	Supplementary requirements	16

6.	acceptance tests and criteria for qualification	16

6.1	Preparation and conditioning of the test specimens	16

6.2	Inspection and selection of the specimens	17

6.2.1	Inspection of thickness	17

6.2.2	Inspection of appearance:	17

6.2.3	Selection	18

6.3	acceptance TESTS AND CRITERIA	18

6.3.1	Identification tests	19

6.3.2	Conformity qualification tests	21

6.3.3	Performance qualification tests	21

6.4	Test report	25

ANNEX I -  DESCRIPTION OF THE SUBSTRATE	26

ANNEX II  GLOBAL DESCRIPTION OF THE PAINT SYSTEM	27

ANNEX III PRODUCT IDENTIFICATION SHEET	28

ANNEX IV TECHNICAL SPECIFICATION FOR APPLICATION OF THE PAINT SYSTEM	30

ANNEX V INSTRUCTIONS FOR USE SHEET	31

ANNEX VI FTIR SPECTRA	33

ANNEX VII SAFETY DATA SHEET	34

# OBJECT

This standard specifies the requirements to be satisfied for the qualification and the approval of fitness for purpose of the protective paint systems designed for the airframes of military aircraft.

These requirements concern:

- the documentation to be provided,

- the performance of the paints,

- the qualification tests and acceptance criteria,

- the paint identification tests.

# SCOPE

This standard applies to paint systems intended for use for coating the exterior surfaces of military aircraft airframes in order to provide:

- protection of metal surfaces against corrosion,

- aerodynamic, aesthetic and stealth functions.

- The standard does not include:

- the following functional characteristics, which are subject to separate qualification:

- anti-erosion,

- electric conduction (antistatic etc.),

- infrared (IR) stealth and radar signature (radar cross-section - RCS),

- resistance to high temperatures.

b) qualification of the following paints:

- paints for interior structures,

- temporary or peelable paints (peel off paints),

- paints for antennas and radomes,

- paints for munitions.

## Types of aircraft

This document concerns all airframes of military aircraft (including drones) belonging to:

- the French army,

- the French fleet air arm (naval aviation),

- The French Army Light Aviation (Aviation Légère de l’Armée de Terre- ALAT),

- the French “gerndarmerie”.

## Types of environment

The selected average atmospheric corrosivity category is C3, as defined in international standard NF EN ISO 12944-2.

## Types of application

The types of application concerned are new build or complete repainting (total refurbishment), which is equivalent to the work of new build.

For regular maintenance operations (spot repairs, touching up etc.), the proposed paint system must be suitable for minor repairs.

## Type of product

Sealing compounds and mastics etc. are not covered by this standard.

## Nature of the substrates and type of surface preparation

a) The substrate types consist of the materials used by aircraft manufacturers for the production of military aircraft airframes:

- steels,

- aluminium alloys, series 2000, 5000, 6000, 7000 and foundry alloys (AlSiMg-type), conforming to standards NF EN 515 and NF EN 573-1 to NF EN 573-4,

- titanium and titanium alloys,

- magnesium alloys,

- reinforced or non-reinforced organic composite materials (carbon epoxy, glass epoxy etc.)

The qualification tests covered by this document apply only to type 2024 T3 aluminium substrate.

b) The reference standards for surface preparation are specified in the table below:

Table 1 – Surface preparation of substrates

| Criterion | Minimum level | Standard |
| --- | --- | --- |
| Dust | Dust quantity < 2 for a particle size category  2 | ISO 8502-3* |
| Probability of condensation | - Relative humidity ≤ 85 % - Temperature of substrate greater than dew point + 3 °C - Temperature of paint application between +10 °C and +30 °C | ISO 8502-4* |
| Oils and greases | None | --- |
| Soluble salts |  5 µg/cm2 | ISO 8502-6 and 9* |

(*) Even though these standards are intended for assessing steel surfaces, they can also be used for other types of substrates commonly found in the aviation domain.

# NORMATIVE REFERENCES

The normative references below are those that should be taken into account for the application of this document.

| Reference | Title |
| --- | --- |
| NF EN 515 | Aluminium and Aluminium alloys – Wrought products – Temper designations. |
| NF EN 573-1 | Aluminium and Aluminium alloys – Chemical composition and form of wrought products. Part 1: Numerical designation |
| NF EN 573-2 | Aluminium and Aluminium alloys – Chemical composition and form of wrought products. Part 2: Chemical symbol based designation system |
| NF EN 573-3 | Aluminium and Aluminium alloys – Chemical composition and form of wrought products. Part 3: Chemical composition. |
| NF EN 573-4 | Aluminium and Aluminium alloys – Chemical composition and form of wrought products. Part 4: Forms of products. |
| ISO 760 | Determination of water — Karl Fischer method (General method) |
| EN ISO 1513 | Paints and varnishes — Examination and preparation of test samples |
| NF EN ISO 1514 | Paints and varnishes– Standard panels for testing |
| EN ISO 1517 | Paints and varnishes -- Surface-drying test -- Ballotini method. |
| NF EN ISO 1518 | Paints and varnishes– Scratch test. |
| NF EN ISO 1519 | Paints and varnishes — Bend test (cylindrical mandrel) |
| NF EN ISO 1520 | Paints and varnishes– Cupping test. |
| ISO 1524 | Paints, varnishes and printing inks -- Determination of fineness of grind. |
| NF EN 2101 | Chromic acid anodizing of aluminium and wrought aluminium alloys |
| EN ISO 2114 | Plastics (polyester resins) and paints and varnishes (binders) – Determination of partial acid value and total acid value. |
| NF EN ISO 2409 | Paints and varnishes– Cross-cut test |
| NF EN ISO 2431 | Paints and varnishes - Determination of flow time by use of flow cups. |
| NF EN 2434-5 | Aerospace series - Paints and varnishes - Two component cold curing polyurethane finish Part 5: High flexibility and chemical agent resistance for military application |
| NF EN 2435-5 | Paints and varnishes. Corrosion resistant chromated two component cold curing primer Part 5: High corrosion resistance for military application |
| NF EN 2436-6 | Aerospace series - Paints and varnishes - Corrosion resistant chromate-free two component cold curing epoxy primer Part 6: High corrosion resistance for military application |
| ISO 2718 | Standard layout for a method of chemical analysis by gas chromatography |
| NF EN ISO 2808 | Paints and varnishes– Determination of film thickness. |
| NF EN ISO 2810 | Paints and varnishes– Natural weathering of coatings– Exposure and assessment |
| NF EN ISO 2811-1 | Paints and varnishes– Determination of density. Part 1: Pycnometer method. |
| NF EN ISO 2812-2 | Paints and varnishes– Determination of resistance to liquids. Part 2: Water immersion method |
| NF EN ISO 2813 | Paints and varnishes -- Determination of specular gloss of non-metallic paint films at 20 degrees, 60 degrees and 85 degrees |
| NF EN ISO 2884-1 | Paints and varnishes - Determination of viscosity using rotary viscometers Part 1: Cone-and-plate viscometer operated at a high rate of shear |
| NF EN ISO 2884-2 | Paints and varnishes - Determination of viscosity using rotary viscometers Part 2: Disc or ball viscometer operated at a specified speed |
| NF EN ISO 3001 | Plastics – Epoxy compounds – Determination of epoxy equivalent. |
| NF EN ISO 3011 | Rubber- or plastics-coated fabrics — Determination of resistance to ozone cracking under static conditions |
| NF EN 3212 | Paints and varnishes - Corrosion test by alternate immersion in a buffered sodium chloride solution Aerospace series |
| NF EN ISO 3251 | Paints, varnishes and plastics– Determination of non-volatile-matter content. |
| ISO 3270 | Paints and varnishes and their raw materials — Temperatures and humidities for conditioning and testing |
| NF EN 3665 | Test methods for paints and varnishes - Filiform corrosion resistance test on aluminium alloys |
| NF EN ISO 3668 | Paints and varnishes– Visual comparison of colour of paints |
| NF EN ISO 3678 | Paints and varnishes – Print free test. |
| NF EN ISO 3679 | Determination of flash point – Rapid equilibrium closed cup method. |
| NF EN ISO 3680 | Determination of flash/no flash — Rapid equilibrium closed cup method. |
| EN 3840 | Aerospace series - Paints and varnishes - Technical specification |
| EN 3847 | Aerospace series - Paints and varnishes - Determination of sedimentation rating |
| EN 4160 | Aerospace series - Paints and varnishes - Determination of the effect of thermal exposure |
| EN 4170 | Aerospace series - Paints and varnishes - Test method for measurement of resistance to cold crack temperature cycle |
| EN 4171 | Aerospace series - Paints and varnishes - Test method for determination of phosphoric acid index |
| EN 4592 | Aerospace series - Paints and varnishes - Test method for determination of infrared reflectance |
| NF EN ISO 4618 | Paints and varnishes– Terms and definitions for paint products |
| NF EN ISO 4628-1 | Paints and varnishes– Evaluation of degradation of coatings– Designation of quantity and size of defects, and of intensity of uniform changes in appearance. Part 1: General introduction and designation system |
| NF EN ISO 4628-2 | Paints and varnishes– Evaluation of degradation of coatings– Designation of quantity and size of defects, and of intensity of uniform changes in appearance. Part 2: Assessment of degree of blistering |
| NF EN ISO 4628-4 | Paints and varnishes– Evaluation of degradation of coatings– Designation of quantity and size of defects, and of intensity of uniform changes in appearance. Part 4: Assessment of degree of cracking |
| NF EN ISO 4628-5 | Paints and varnishes– Evaluation of degradation of coatings– Designation of quantity and size of defects, and of intensity of uniform changes in appearance. Part 5: Assessment of degree of flaking |
| NF EN ISO 4628-8 | Paints and varnishes– Evaluation of degradation of coatings– Designation of quantity and size of defects, and of intensity of uniform changes in appearance. Part 8: Assessment of degree of delamination and corrosion around a scribe or other artificial defect |
| NF EN ISO 4629 | Binders for paints and varnishes — Determination of hydroxyl value — Titrimetric method .. |
| NF EN ISO 6270-1 | Paints and varnishes– Determination of resistance to humidity. Part 1: Continuous condensation |
| ISO 6286 | Molecular absorption spectrometry — Vocabulary — General — Apparatus |
| NF EN ISO 8502-3 | Preparation of steel substrates before application of paints and related products -- Tests for the assessment of surface cleanliness. Part 3: Assessment of dust on steel surfaces prepared for painting (pressure-sensitive tape method) |
| NF EN ISO 8502-4 | Preparation of steel substrates before application of paints and related products -- Tests for the assessment of surface cleanliness. Part 4: Guidance on the estimation of the probability of condensation prior to paint application |
| NF EN ISO 8502-6 | Preparation of steel substrates before application of paints and related products -- Tests for the assessment of surface cleanliness. Part 6: Extraction of soluble contaminants for analysis -- The Bresle method |
| NF EN ISO 8502-9 | Preparation of steel substrates before application of paints and related products -- Tests for the assessment of surface cleanliness. Part 9: Field method for the conductometric determination of water-soluble salts |
| NF EN ISO 9000 | Quality management systems – Essential principles and vocabulary. |
| NF EN ISO 9001 | Quality management systems – Requirements. |
| NF ISO 9223 | Corrosion of metals and alloys — Corrosivity of atmospheres — Classification, determination and estimation |
| NF EN ISO 9227 | Corrosion tests in artificial atmospheres – Salt spray tests. |
| EN ISO 9514 | Paints and varnishes -- Determination of the pot life of multicomponent coating systems -- Preparation and conditioning of samples and guidelines for testing |
| EN ISO 9702 | Plastics — Amine epoxide hardeners — Determination of primary, secondary and tertiary amine group nitrogen content |
| NF EN ISO 11507 | Paints and varnishes– Exposure of coatings to artificial weathering - Exposure to fluorescent UV lamps and water. |
| NF EN ISO 11890-1 | Paints and varnishes– Determination of volatile organic compound (VOC) content. Part 1: Difference method. |
| NF EN ISO 11890-2 | Paints and varnishes– Determination of volatile organic compound (VOC) content. Part 2: Gas-chromatographic method. |
| NF EN ISO 11909 | Binders for paints and varnishes — Polyisocyanate resins — General methods of test |
| NF EN ISO 12944-1 | Paints and varnishes– Corrosion protection of steel structures by protective paint systems. Part 1: General introduction |
| NF EN ISO 12944-2 | Paints and varnishes– Corrosion protection of steel structures by protective paint systems. Part 2: Classification of environments |
| NF EN ISO 14680-1 | Paints and varnishes - Determination of pigment content. Part 1: Centrifuge method. |
| EN ISO 15528 | Paints, varnishes and raw materials for paints and varnishes — Sampling |
| NF EN ISO 17872 | Paints and varnishes - Guidelines for the introduction of scribe marks through coatings on metallic panels for corrosion testing |
| NF EN ISO 19840 | Paints and varnishes– Corrosion protection of steel structures by protective paint systems– Measurement of, and acceptance criteria for, the thickness of dry films on rough surfaces |
| NF EN ISO 29117 | Determination of through-dry state and through-dry time |
| NF X 08-012-1 | Colours - Colorimetry - Colorimetric characteristics of coloured samples Part 1: Definitions and basic assessment principles |
| ND X08-012-2 | Colours - Colorimetry - Colorimetric characteristics of coloured samples Part 2: Practical considerations concerning instrumentation and reflection measurement |
| NF T 30-050 | Determination of flash point in closed cup test with stirring. |
| NF T 36-005 | Paints and varnishes– Classification of paints, varnishes and associated products |
| NORMDEF 0001 | National defence colours. |
| AEP 64 STANAG 4360) | Performance requirements for paint systems resistant to chemical agents and decontaminants, for the protection of land military equipment |
| AEP 65 STANAG 4360) | Performance requirements and test method for paint systems resistant to chemical warfare agents |
| MIL-PRF-85285 | Performance specification coating: polyurethane, aircraft and support equipment |

The users of these documents must regularly verify the validity of the copies in their possession by consulting the bodies responsible for their distribution:

# TerminologY AND abBREViations

## Terminology

a)This standard uses terms specific to the paint industry. This vocabulary, which usually has a specific use in this technical area, is always used in a general sense. Consequently, no reminder of vocabulary meanings is necessary.

b) The terms and definitions specific to the technical field of paint systems are given in international standard NF EN ISO 4618..

c) However, it is worth reiterating the definitions of the following two distinct notions:

- Surface preparation (SP): process that does not alter the nature of the surface of the substrate material. Examples: degreasing (solvent-based detergent), chemical or mechanical stripping

- Surface treatment (ST): procedure that alters the nature of the surface of the substrate material. Examples: chromating, anodizing of aluminium

## Abbreviations

ALAT: 	Aviation Légère de l’Armée de Terre (Army Light Aviation)

SG:	Specular Gloss

CLP:	Classification, Labelling, Packaging

CMR:	Carcinogenic, Mutagenic, Reprotoxic

VOC:	Volatile Organic Compound

DDP:	Dossier de Définition Peinture (Paint definition file)

DDS:	Dossier de Définition du Système de peinture (Paint system definition file)

FC:	Correction Factor

SDS:	Safety Data Sheet

IR:	InfraRed

FTIR:	Fourier Transform InfraRed

OAC: 	Chromic Anodic Oxidation

NIR:	Near InfraRed

SP: 	Surface Preparation

RCS:	Radar Cross-Section

REACh :	Registration Evaluation and Authorization of Chemicals

ST: 	Surface Treatment

TLV-STEL:	Threshold Limit Value - Short-Term Exposure Limit

TLV:	Threshold Limit Value

# Prerequirements for qualification

## Documentation requirements:

A set of reference documentation must be established for each paint system; this reference base must comprise the following information and documents:

- Description of the substrate (SP and/or ST) (see Annex II);

- General Technical Specification of the paint system (see Annex II);

- Identification Sheet of the products, drawn up for each component and for the ready-to-use mixture (see Annex III);

- Technical Specification for the application of the paint system (see Annex IV);

- Instructions for Use sheet (see Annex V),

- FTIR spectra (see Annex VI) ;

- Safety Data Sheets (SDS) of the supplied products in conformity with the provisions of the REACH regulation (Article 31) (see Annex VII).

Any variation in the chemical composition of a preparation that forms part of the paint system must be notified and duly explained by the manufacturer, which must provide evidence that this change has no impact on the expected performance of the system.

## Requirements of the paint products

### Type of product

The types of product used are solvent based or non-solvent based paints that can be applied by brush, roller, spray gun or automated system and that dry at ambient temperature under normal workshop conditions.

The product components must comply with the regulations in force (REACH, VOC directives etc.)

- Flash point: liquid paints are required to have a flash point:

- greater than or equal to 21°C for solvent based paints,

- greater than or equal to 55°C for aqueous phase paints.

- Volatile Organic Components (VOC): to reduce VOC emissions caused by the use of organic solvents in certain paints and varnishes, the VOC content of the paints must be as low as possible. With reference to military standard MIL-PRF-85285E, the paint systems can be classified as follows:

- Type I, class H: finishing paint with high non-volatile matter content, if VOC ≤ 420 g/l,

- Type III, class W: water-thinnable or aqueous phase paint,

- Conventional finishing paint with solvents.

The VOC content of paints (including the solvents necessary for thinning operations), established in accordance with international standard NF EN ISO 11890-1 or 2, depending on the VOC concentration, must be clearly stated in the Safety Data Sheet (SDS) of the products.

The colour of the applicable paint systems is defined in French Defence standard NORMDEF 0001.

Qualification relates to the following shades:

- medium grey 3630, considered representative of standard aircraft colours;

- NIR dark green 34X3, considered representative of the “special” colours.

### Durability

The protective paint system must have resistance characteristics compatible with the maintenance cycles of military aircraft. The required durability is Type H “High Durability” (more than 15 years) as defined in NF EN ISO 12944-1.

During a period of at least 10 years, the paint system must not require any total refurbishment; only spot repairs of the type performed in regular maintenance are permissible.

### Regulatory constraints (environment, health and safety)

The paints must:

- be applicable in compliance with the legislation in force in Europe concerning VOCs;

- not contain any components prohibited by the legislation in force.

New formulations must;

- comply with the REACh regulation;

- have a label that complies with the legislation in force and must have Heath, Safety and Environmental impact no greater than the indications specified in their SDS:

### General requirements

The paint systems proposed for qualification must:

- be suitable for spot repairs;

- be compatible with the paint systems on the aircraft currently in service;

- be strippable either by mechanical means (light sanding, blast cleaning etc.) or by chemical means;

The application of the paints constituting the system must take into account the following conditions:

- The normal application and drying conditions prevailing in a paint application shop (temperature between 10 °C  and 30 °C and relative humidity between 30 % et 75 %) ;

- the use of conventional paint application equipment (brush, low-pressure spray gun);

- a pot life greater than or equal to 2h at a temperature of \23 °C;

- a minimum recoat time of less than 2 hours for a temperature of 23 °C.

- a storage time of at least 12 months (after delivery);

- a physical and chemical condition that, at the time of delivery or during storage, is free of skins, particles, hard sediments or irreversible phase separation

### Constitution of the paint system applied to exterior surfaces

The paint system must comprise a minimum of one primer coat and one finishing coat.

The thickness of the complete system must be:

- a minimum of 60 µm;

- a maximum of 200 µm.

### Supplementary requirements

#### CMR substances of Category 1 or 2 (Directive 67/548/EC) or Category 1A or 1B (Regulation 1272/2008)

The paint products must not contain carcinogenic, mutagenic or reprotoxic (CMR) substances classified in categories 1 or 2 (Directive 67/548/EC), or categories 1A or 1B (Regulation No. 1272/2008), according to the following risk phrases:

- R45, R46, R49, R60, R61 (Directives 67/548/EC and 1999/45/CE concerning respectively the classification, packaging and labelling of substances and preparations);

- H340, H350, H350i, H360d, H360f (Regulation No. 1272/2008,  known as the “CLP Regulation” (Classification, Labelling, Packaging) concerning the classification, labelling and packaging of chemical substances and mixtures, which shall repeal directives 67/548/EC and 1999/45/EC).

#### CMR substances Category 3 (Directive 67/548/EC) or Category 2 (Regulation 1272/2008)

The paint products must not contain CMR substances classified in Category 3 (Directive 67/548/EC) or Category 2 (Regulation No. 1272/2008) according to the following risk phrases:

- R40, R62, R63, R68 (Directives 67/548/EC and 1999/45/CE concerning respectively the classification, packaging and labelling of substances and preparations);

- H341, H351, H361d, H361f (Regulation No. 1272/2008, known as the “CLP Regulation” concerning the Classification, Labelling, and Packaging of chemical substances and mixtures, which shall repeal directives 67/548/EC and 1999/45/EC).

#### Short-Term Exposure Limit and Threshold Limit Value

The use of substances with no Short-Term Exposure Limit (TLV-STEL) and Threshold Limit Value (TLV) is strongly recommended. Substances subject to TLV and TLV-STEL must be specified in the SDS of the products.

# acceptance tests and criteria for qualification

## Preparation and conditioning of the test specimens

The test specimens are defined below.

Table 2 -Preparation and conditioning of the test specimens

| Subject | Value / Instruction | Observations |
| --- | --- | --- |
| Type of substrate | Aluminium alloy2024 T3 | Chromic acid oxidation (CAO, without sealing, in accordance with standard EN 2101 Test specimens in accordance with standard ISO 1514 |
| Dry film thickness | Conforming to the thickness defined in section. 6.2.1 |  |
| Conditioning | Lab temperature: 23 ± 2 °C | Minimum 3 weeks conditioning before conducting the tests |
| Scratches | Salt spray tests | See table in section 6.2.3 |
| Application | Conforming to the data in the data sheets of the paint system and constituent paints | See Annexes I and II |

## Inspection and selection of the specimens

Acceptance of the test specimens shall be declared after checking two parameters, thickness and appearance.

### Inspection of thickness

Thickness inspection on rough substrates must include the dead volume in accordance with NF EN ISO 19840, which specifies two methods of calibrating the measuring apparatus:

	Calibration of the apparatus on a smooth shim: in this case the roughness must be taken into account by applying a correction factor (FC):

 Thickness = value given by the apparatus – correction factor

(where FC = 10 µm if the roughness is “fine” as defined in standard NF EN ISO 8503)

	Calibration on the ready-to-paint surface: in this case, no correction factor is required to allow for surface roughness.

The total thickness of the dry film or the thickness of each coat constituting the paint system is determined by the mean value obtained from a minimum number of measurements depending on the surface area of the specimens.

- for test specimens with an area of less than 100 cm2: 3 measurements;

- for test specimens with an area between 100 and 500 cm2: 10 measurements;

- for test specimens with an area greater than 500 cm2: 20 measurements.

The thicknesses of the primer coat are directly measured. The thickness(es) of the finishing coat(s) is (are ) calculated by the difference between the total thickness and the mean thickness of undercoats(s).

The results must conform to the results below for a series of measurements (on test specimens).

Table 3 - Requirements and tolerances for the thickness of paint coats

| Recommended nominal thickness (e) in µm | Tolerance on the mean thickness in µm | Tolerance on the maximum thickness in µm |
| --- | --- | --- |
| 60< e ≤ 100 | e mean = e ± 20 | e mean = e ± 30 |
| 100< e< 200 | e mean = e ± 30 | e mean = e ± 40 |

In addition to the requirements on the mean and maximum thickness, the complete dry film must satisfy the conditions below:

- Smallest measured value: greater than 60 µm

- Largest measured value: less than  200 µm

### Inspection of appearance:

This inspection is conducted in accordance with NF EN ISO 4628-1 to 4. The characteristics defined in the table below are evaluated visually:

- Table 4– Inspection of appearance

| Characteristic of the appearance | Standard | Measurements |
| --- | --- | --- |
| Any flaw in the appearance or arising from problems of compatibility: Orange peel, wrinkling , etc. | NF EN ISO 4628-1 to 4 | Evaluation of degradation of coatings – Designation of quantity and size of defects, and of intensity of uniform changes in appearance |

The results must comply with the requirements given in the table below:

- Table 5– Requirements

| Type of system | Requirement |  |
| --- | --- | --- |
|  | Orange peel, wrinkling, pinholing, grits and dust, cratering, blistering, flaking, cracking, etc. | Appearance |
| Base system | Quantity of defects: 0 Size of defects: 0 | No major variation in gloss or colour on visual examination of the surface of the specimen |
| High temperature system |  |  |
| Non-skid system for personnel, coated with the finishing coat |  |  |

### Selection

Only specimens that comply with the 2 criteria above (thickness and appearance) shall be selected for the laboratory tests.

## acceptance TESTS AND CRITERIA

The majority of the proposed tests and the quantity of tests conform to European standard EN 3840; the test number specified in this standard is entered in the first column, except in the case of the artificial weathering tests, which is conducted in accordance with ISO 11507 Some tests are not adopted, but certain other tests have been introduced.

The test specimens used for analysis must be representative of the product. Unless otherwise specified in the material specification or the normative reference for the test method, the products must be sampled and prepared in conformity with standards EN ISO 15528 and EN ISO 1513.

Three test categories are specified:

- identification tests,

- conformity qualification tests,

- performance qualification tests.

### Identification tests

The tests are defined in the table below:

- Table 6 – Identification test

| No. | Type | Reference standards | Base | Hardener | Mixture | Manufacturer’s values |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Non-volatile matter content (%) | NF EN ISO 3251 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 | ± 2 % of the reference value | ± 2 % of the reference value |  | Specification to be defined by the manufacturer |
| 2 | Pigment content (%) | NF EN ISO 14680-1 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  | Specification to be defined by the manufacturer |
| 3 | Density (g/cm3) | NF EN ISO 2811-1 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 | ± 2 % of the reference value | ± 2 % of the reference value |  | Specification to be defined by the manufacturer |
| 5 | Sedimentation index (ml/4 h) | EN 3847 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  | Specification to be defined by the manufacturer |
| 7 | Flash point (°C) | NF EN ISO 3679 or 3680 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 | ≥ reference value | ≥ reference value |  | Specification to be defined by the manufacturer |
| 8 | Flow time (s) | NF EN ISO 2431 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  | ± 10 % of the reference value | Specification to be defined by the manufacturer |

| 9 | Viscosity at high rate of shear (in Pa.s or in mPa.s) | NF EN ISO 2884-1 or 2884-2 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  | Specification to be defined by the manufacturer |
| --- | --- | --- | --- | --- | --- | --- |
| 10 | Fineness of grind (µm) | NF ISO 1524 NF EN 2434-5, NF EN 2435-5 NF EN 2436-6 | ≤ 30 µm | ≤ 30 µm |  | Criteria to be discussed with the manufacturer |
| 11 | Determination of composition by gas chromatography (%) | ISO 2718 NF EN 2434-5, NF EN 2435-5 NF EN 2436-6 |  |  |  |  |
| 12 | Determination of composition by gas spectrometry (%) | ISO 6286 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 13 | Water content (%) | ISO 760 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 14 | Amine content (%) | EN ISO 9702 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 15 | Hydroxide content (%) | NF EN ISO 4629 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 16 | Isocyanate content (%) | NF EN ISO 11909 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 17 | Epoxy content (%) | NF EN ISO 3001 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 18 | Acid content (%) | EN ISO 2114 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |
| 19 | Phosphoric acid content (%) | EN 4171 NF EN 2434-5, NF EN 2435-5, NF EN 2436-6 |  |  |  |  |

### Conformity qualification tests

The tests are defined in the table below:

- Table 7 – Conformity qualification test

| No. | Description | Reference standards | Criteria |
| --- | --- | --- | --- |
| 20 | Pot life (h) | EN ISO 9514 | Reference value on manufacturer’s representative product |
| 21 | Surface drying time (h) | EN ISO 1517 | Reference value on manufacturer’s representative product |
| 22 | Controllable drying time (h) | NF EN ISO 3678 | Reference value for manufacturer’s representative product |
| 23 | Through-dry time (h) | NF EN ISO 29117 | Reference value for manufacturer’s representative product |
| 27 | Specular gloss (SG) in % | NF EN ISO 2813 | In accordance with NORMDEF 0001, conforming to qualification shade DEF 3630 and 34X3 |
| 30 | Colour measurement: - Visual - Colorimetry | NF EN ISO 3668 NF X 08-012 | In accordance with NORMDEF 0001, conforming to qualification shade DEF 3630 and 34X3 |
| 31 | IR Reflectance | EN 4592 | In accordance with NORMDEF 0001, conforming to qualification shade DEF 34X3 |
| 49 | VOC (g/l) | NF EN ISO 11890-1 or -2 | Reference value on manufacturer’s representative product |

### Performance qualification tests

#### Definition of the tests

These tests are defined in the tables below:

- Table 8 – Performance qualification test

| No. | Designation | Reference standards | Test specimens | Acceptance criteria |
| --- | --- | --- | --- | --- |
| 24 | Initial cross-cut test after 7 days drying, at 23 ± 2 °C | NF EN ISO 2409: adhesive tape method (see Annex A.2) with adhesive strength = 7 ± 0,2 N/cm | Thickness between 0.6 and 1.6 mm | Classification  1 |
| 25 | Bend test (cylindrical mandrel): - mandrel diameter 8 mm, at ambient temperature (23°C) - mandrel diameter 45 mm, at -50 °C | ISO 1519 | Thickness 0.6 mm | - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 |
| 29 | Scratch resistance | NF EN ISO 1518 | Thickness between 0.6 and 1.6 mm | > 1500 g, for test conditions conforming to ISO 3270 |
| 34 | Water resistance, 40°C / 168h | EN ISO 2812-2 | Thickness between 0.6 and 1.6 mm | - tests 24 :  1 - test 29 : > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - Eab* < 1 (colorimetric deviation on the test specimen before and after the test) |
| 35 | Resistance to fluids Fuel: F34 Oil: type O-159 Hydraulic fluid: Skydrol LD4 De-icing fluid | Common exposure duration 7 days Exposure temperature: - 23 °C (ambient) - 70 °C - 70 °C - 23 °C | Thickness between 0.6 and 1.6 mm | - test 24:  1 - test 29: > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - Eab* < 1 (colorimetric deviation3 on the test specimen before and after the test) - test 25: compliance with the criteria of test 25 |

| 36 | Resistance to temperature cycle, 20 cycles at –40 °C to +80 °C | EN 4170 (Tmin -40 °C instead of –55 °C) | Thickness between 0.6 and 1.6 mm | - test 24:  1 - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - Eab* < 1 (colorimetric deviation3 on the test specimen before and after the test) - test 25 at 23°C: compliance with the criteria of test 25 |
| --- | --- | --- | --- | --- |
| 37 | Resistance to humidity - continuous condensation 40 °C / 95 %RH / 500 h | EN ISO 6270-1 | Thickness between 0.6 and 1.6 mm | - tests 24:  1 - test 29: > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - Eab* < 1 (colorimetric deviation3 on the test specimen before and after the test) - test 25 at 23°C: compliance with the criteria of test 25 |
| 38 | Thermal exposure (150 °C / 24 h) | EN 4160 | Thickness between 0.6 and 1.6 mm | - tests 24:  1 - test 29: >1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - test 25 at 23°C: compliance with the criteria of test 25 |
| 39 | Resistance to natural weathering, 2 years at corrosivity class C3 (see. NF EN ISO 12944-2) | NF EN ISO 2810 | Thickness between 0.6 and 1.6 mm Scratch:. See section 6.2.3.2 of the standard | - filament length < 1.5 mm in accordance with NF EN ISO 4628-8 - tests 24:  1 - test 29: > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - Eab* < 1 (colorimetric deviation3 on the test specimen) - test 25 at 23°C: compliance with the criteria of test 25 before and after the test) |
| 40 | Resistance to artificial weathering: Tests at UVA = 340 nm, with a test duration of 1008 hours (126 cycles) | NF EN ISO 11507 – method A | Thickness between 0.6 and 1.6 mm | - Eab* < 1 (colorimetric deviation3 on the test specimen before and after the test) - tests 24:  1 - test 29: > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 - test 25: compliance with the criteria of test 25 |
| 41 | Alternate immersion (NaCl à 3 % g/g, 35 °C during 1500 h) | NF EN 3212 | Thickness between 0.6 and 1.6 mm | - tests 24:  1 - test 29: > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - corrosion less than 1.5 mm |
| 42 | Neutral salt spray (3000 h) | NF EN ISO 9227 (§ 3.2) | Thickness between 0.6 and 1.6 mm Scratch:. See section 6.2.3.2 of the standard | - tests 24:  1 - test 29: > 1500 g - no blistering (NF EN ISO 4628-2), degree = 0 - corrosion less than 1.5mm 1.5 mm in accordance with NF EN ISO 4628-8 |
| 43 | Filiform corrosion (40°C, 82% RH / 1000 hours) | NF EN 3665 | Thickness between 0.6 and 1.6 mm | - No blistering (NFEN ISO 4628-2), degree = 0 - corrosion less than 2 mm |
| 46 | Slow deformation: ≤ 5 mm | NF EN ISO 1520 | ISO 1520 | - no blistering (NF EN ISO 4628-2), degree = 0 - no cracking (NF EN ISO 4628-4), degree = 0 - no flaking (NF EN ISO 4628-5), degree = 0 |
| 52* | Resistance to chemical agents | AEP 65 |  | In conformity with NATO publication AEP 65 |
| 53* | Resistance to decontamination | AEP 64 with Q2000 solution |  | In conformity with NATO publication AEP 64 |

* optional tests, depending on the functionality of the paint and if selected; tests conducted by the DGA.

Note: For standards NF EN ISO 4628-2, 4628-4 and 4628-5, the notion of “no blistering (cracking or flaking)” equivalent to degree 0 of the evaluation.

#### Coating scratch method for tests 39 and 42

The coating scratch on the test specimen must conform to Figure 1 and must expose the bare substrate. The tool used for the scratch should be a single blade cutting tool (For further details, please refer to standard NF EN ISO 17872 “Paints and varnishes - Guidelines for the introduction of scribe marks through coatings on metallic panels for corrosion testing”). The scribe mark must either have parallel sides or a widening towards the top, exposing the bare metal substrate over a width of approximately 0.5 mm (eliminate all debris from around the scratch).

(L-100mm)/2

lg/4

L

Scratch.

lg

Figure 1: Size and position of scratch

## Test report

At the end of the qualification programme described in this document, the test report must provide both individual reports conforming to the standard applicable to each of the specified tests, and an overall summary of all the test results obtained.

The report must precisely identify all of the test specimens, all of the deviations from the analysis methods described, the operating details not laid down in the documentation and any incidents that have occurred at any time during the qualification procedure.

- DESCRIPTION OF THE SUBSTRATE

|  |  | SUBSTRATE 1 | SUBSTRATE 2 |
| --- | --- | --- | --- |
| SUBSTRATE | Material designation: |  |  |
|  | Standardised grade: |  |  |
|  | Quality / State: |  |  |
|  | Thickness: |  |  |
| SURFACE PREPARATION (*) | Type: |  |  |
|  | Detailed description (products and/or abrasives used, methodology, etc.) |  |  |
|  | Characteristics to be obtained for the surface state (degree of cleanliness, roughness, dusts, soluble salts, etc.): |  |  |
| SURFACE TREATMENT (**) | Type: |  |  |
|  | Detailed description (products used, methodology, etc.) |  |  |
|  | Characteristics to be obtained for the surface state (coating weight, etc.): |  |  |

(*) Surface preparation (SP): process that does not alter the nature of the surface of the substrate material. Example: cleaning (solvent, detergent), chemical stripping, heat stripping (burning) or mechanical stripping (high pressure cleaning, abrasive projection).

(**) Surface treatment (ST): process that alters the nature of the surface of the substrate material. Example: phosphating, chromating, anodising of aluminium, thermo-chemical diffusion treatment

- GLOBAL DESCRIPTION OF THE PAINT SYSTEM

(Tick the relevant box)

| O Basic paint system | O Exterior European Theatre O Exterior for aviation applications |
| --- | --- |

- PRODUCT IDENTIFICATION SHEET

 For liquid products

| Manufacturer's Logo | PRODUCT IDENTIFICATION |  |  | Date of issue |  | Page |
| --- | --- | --- | --- | --- | --- | --- |
| PRODUCT (complete designation and reference): |  |  |  |  |  |  |
| FORMULATION: |  | CLASSIFICATION: |  |  |  |  |
| Index: |  | AFNOR (in accordance with NF T 36-005) |  |  | NATO |  |
| Date: |  | Family: | Category: |  |  |  |
|  |  | Manufacturer’s details (*) |  |  | Reference of the standard used |  |
|  |  | Component A (base) | Component B (hardener) |  |  |  |
| Colour (Ref. AFNOR, RAL or other) |  |  |  |  |  |  |
| Liquid product: |  |  |  |  |  |  |
| Non-volatile matter content (%) |  |  |  |  | NF EN ISO 3251 |  |
| Pigment content (%) |  |  |  |  | NF EN ISO 14680 |  |
| Density (g/cm3) |  |  |  |  | NF EN ISO 2811 |  |
| Sedimentation index (ml/4 h) |  |  |  |  | NF EN ISO 3847 |  |
| Flash point (°C) |  |  |  |  | NF EN ISO 3679 or 3680 |  |
| Flow time (s) |  |  |  |  | NF EN ISO 2431 |  |
| Viscosity at high rate of shear (in Pa.s or in mPa.s) |  |  |  |  | NF EN ISO 2884-1 |  |
| Fineness of grind (µm) |  |  |  |  | NF ISO 1524 |  |
| Determination of composition by gas chromatography (%) |  |  |  |  | ISO 2718 |  |
| Determination of composition by gas spectrometry (%) |  |  |  |  | ISO 6286 |  |
| Water content (%) |  |  |  |  | ISO 760 |  |
| Amine content (%) |  |  |  |  | EN ISO 9702 |  |
| Hydroxide content (%) |  |  |  |  | NF EN ISO 4629 |  |
| Isocyanate content (%) |  |  |  |  | NF EN ISO 11909 |  |
| Epoxy content (%) |  |  |  |  | NF EN ISO 3001 |  |
| Acid content (%) |  |  |  |  | EN ISO 2114 |  |
| Phosphoric acid content (%) |  |  |  |  | EN 4171 |  |

(*) For two-component products, complete in two columns where applicable. Whatever the case, do not provide the data for the component mixture

 For powder products

| Manufacturer's Logo | PRODUCT IDENTIFICATION |  |  | Date of issue |  | Page |
| --- | --- | --- | --- | --- | --- | --- |
| PRODUCT (complete designation and reference): |  |  |  |  |  |  |
| FORMULATION: |  | CLASSIFICATION: |  |  |  |  |
| Index: |  | AFNOR (in accordance with NF T 36-005) |  |  | NATO |  |
| Date: |  | Family: | Category: |  |  |  |
|  |  | Manufacturer’s details (*) |  |  | Reference of the standard used |  |
|  |  | Component A (base) | Component B (hardener) |  |  |  |
| Colour (Ref. AFNOR, RAL or other) |  |  |  |  |  |  |
| Powder product: |  |  |  |  |  |  |
| Density |  |  |  |  | NF T 30-505 |  |
| Capacity to fluidify |  |  |  |  | NF T 30-501 |  |
| Agglomeration temperature |  |  |  |  | NF T 30-502 |  |
| Gelling time |  |  |  |  | NF T 30-506 |  |
| Determination of the mass loss on heating |  |  |  |  | NF T 30-503 |  |

(*) For two-component products, complete in two columns where applicable. Whatever the case, do not provide the data for the component mixture

- TECHNICAL SPECIFICATION FOR APPLICATION OF THE PAINT SYSTEM

| TECHNICAL SPECIFICATION FOR APPLICATION OF THE PAINT SYSTEM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Manufacturer's Logo |  | NAME: |  |  |  |  |  |  |  |  |  |  |  | SHEET N°: |  |  |  |  |  |  |  |  |
|  |  | DESCRIPTION: |  |  |  |  |  |  |  |  |  |  |  | VERSION: |  |  |  |  |  |  |  |  |
|  |  | SURFACE PREPARATION: In all cases, the paints must be applied on surfaces that are clean, dry and free of any contaminant as described in ISO 8502. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| COMPOSITION OF THE SYSTEM: |  | Appearance | Number of coats | Thickness of dry film: coat (µm) |  |  | Dry film mass (g/m2/c)  | Nominal application density (g/m2/c) |  | Dry extract density (%) |  | Spreading capacity (m2/l) |  | Anticipated procurement (l/m2/c)  |  | Methods of application  |  |  |  |  |  |  |
| Reference | Reference |  |  | nom. | min. | max. |  |  |  |  |  |  |  |  |  | B | R | P |  | T | E |  |
| CHARACTERISTICS OF THE PAINTS: |  | Contractual thickness (µm): |  |  |  |  |  | Total dry film mass (g/m2): |  |  |  |  |  | Period before commissioning: |  |  |  |  |  |  |  |  |
| Reference | Description |  |  |  |  |  |  | Dried until dry to touch at 20 °C | Recoat time at 20 °C |  |  |  | PLAM at 20°C | Minimum application temperature | Flash point (°C) |  |  |  | Type of thinner, where appropriate |  |  |  |
|  |  |  |  |  |  |  |  |  | min |  | maximum |  |  |  |  |  |  |  |  |  |  |  |
| COMMENTS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  For nominal thickness  Given an average loss of about 30 % (indicative contractual value),  B: Brush, R: Roller, P: Gun, T: Trowel, E: Electrostatic gun,  Pot life after mixing. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

- Instructions for use sheet

| Manufacturer's Logo |  |  |  |  | PAINTS AND VARNISHES STANDARD PRODUCT |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| REFERENCE |  |  |  | PRODUCT: |  |  |  |  |  |  |  |
|  |  |  |  | CLASSIFICATION: |  |  |  |  |  | EDITION: |  |
|  |  |  |  | AFNOR in accordance with NF T 36-005 |  |  | NATO |  |  |  |  |
|  |  |  |  | Family: | Category: |  |  |  |  |  |  |
| SHEET |  |  | C | #### INSTRUCTIONS FOR USE |  |  | PAGE 1/2 |  |  |  |  |
| THIS EDITION CANCELS AND REPLACES THE PREVIOUS EDITION DATED: |  |  |  |  |  |  |  |  |  |  |  |
| Surface preparation |  | Applicable on: |  |  |  |  |  |  |  |  |  |
|  |  | Recoatable by: |  |  |  |  |  |  |  |  |  |
| PHYSICAL-CHEMICAL CHARACTERISTICS |  | PRESENTATION: |  |  |  |  |  |  |  |  |  |
|  |  | Appearance of film: |  |  |  |  |  |  |  |  |  |
|  |  | Density (g/cm3) (NF EN ISO 2811-1) : |  |  |  | Paint: |  |  | Dry film: |  |  |
|  |  | Non-volatile content (dry extract) (%) (NF EN ISO 3251) : |  |  |  | By weight: |  |  | By volume: |  |  |
|  |  | Flash point (°C) |  |  |  | A = |  | B = |  |  | A+B = |
|  |  | NOMINAL CHARACTERISTICS PER COAT: |  |  |  |  |  |  |  |  |  |
|  |  | Film thickness (µm): |  |  |  | Dry: |  |  | Wet: |  |  |
|  |  | Density of unit application: |  |  |  | g/m2 |  |  | l/m2 |  |  |
|  |  | Spreading capacity (m2/l): |  |  |  |  |  |  |  |  |  |
|  |  | Dry film mass (g/m2): |  |  |  |  |  |  |  |  |  |
| THE VALUES ENTERED IN THE BOX ABOVE ARE ROUNDED. |  |  |  |  |  |  |  |  |  |  |  |
|  | INFORMATION ABOUT THE PRODUCT: |  |  |  |  |  |  |  |  |  |  |
|  | Number of litres of solvent vapour released per litre of paint (20°C). |  |  |  |  |  |  |  |  |  |  |
|  | VOC content (g/l): |  |  |  |  |  |  |  |  |  |  |
|  | Presence of CMR Category 3 (Yes/No) : |  |  |  |  |  |  |  |  |  |  |

| Manufacturer's Logo: |  |  |  | PAINTS AND VARNISHES STANDARD PRODUCT |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| REFERENCE |  | PRODUCT: |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | CLASSIFICATION: |  |  |  |  |  |  |  |  | EDITION: |  |  |  |
|  |  | AFNOR in accordance with NF T 36-005 |  |  |  |  | NATO |  |  |  |  |  |  |  |
|  |  | Family: |  | Category: |  |  |  |  |  |  |  |  |  |  |
| SHEET | C | #### INSTRUCTIONS FOR USE |  |  |  |  | PAGE 2/2 |  |  |  |  |  |  |  |
| THIS EDITION CANCELS AND REPLACES THE PREVIOUS EDITION DATED: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| INSTRUCTIONS FOR USE |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mixture ratio: |  |  |  |  | Mass A = |  |  |  |  | Mass B = |  |  |  |  |
|  |  |  |  |  | Volume A = |  |  |  |  | Volume B = |  |  |  |  |
| Preparation before use: |  |  |  |  | Homogenise for a few minutes by mechanical stirring |  |  |  |  |  |  |  |  |  |
| Recommended conditions: |  |  |  |  | Temperature (°C) |  |  |  | min. +5 |  |  |  | max. +40 |  |
| T° substrate > T° dew point +3°C |  |  |  |  | Relative humidity (%): < 85 |  |  |  |  |  |  |  |  |  |
| METHODS OF APPLICATION |  |  |  |  | AIRLESS |  |  | PNEUMATIC |  |  |  | BRUSH/ ROLLER |  |  |
| Viscosity: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Thinning if any: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Thinner: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Achievable thickness (µm): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Nozzle (Ф mm): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Pressure (bar): |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Cleaning solvent: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| APPLICATION TEMPERATURE |  |  |  |  | 10 °C |  |  | 20 °C |  |  |  | 35 °C |  |  |
| Usability period after mixing: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Drying time for nominal thickness: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| dry dust-free |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| dry to touch |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Recoat time min. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| max. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| DRYING METHODS: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CONDITIONING: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| STORAGE: |  |  | Store at a temperature between +5 °C and +35 °C |  |  |  |  |  |  |  |  |  |  |  |
| STABILITY: |  |  | 18 months minimum (starting from the delivery date) in a sheltered location, under the storage conditions specified above and in the sealed original packaging. Additionally, check the technical characteristics of the paint before - using. |  |  |  |  |  |  |  |  |  |  |  |
| OBSERVATIONS: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

- FTIR SPECTRA

The FTIR (Fourier transform infra-red) spectra between 250 nm and 2500 nm of each component (base + hardener) of each paint system must be provided by the manufacturer.

These spectra serve as the reference spectra and must be accompanied by a sworn declaration, signed by the company’s delegated corporate officer, who must declare that he/she personally guarantees their compliance.

- SAFETY DATA SHEETS

Safety data sheets (SDS) must be provided for each of the constituent products of the paint system. The provided standard form for safety data sheets complies with the REACH regulation.

These sheets are the responsibility of the paint manufacturer.

The users of a product must check the validity of the safety data sheet in their possession.



\The texts of these reference standards have been identified by critical choices as the most suitable for defining the general requirements for the paint systems specified in this document.

(?) : 10 °C or the minimum recommended value, which will also be specified in the table in Annex V – Instructions for Use.

: Eab* is the global colorimetric deviation (or colour difference) in the CIELAB colour space.. Its calculation formula is: Eab*  = [(L*)2 + (a*)2 + (b*)2]1/2 where L* is the CIE 1976 difference in lightness (in the CIELAB colour space).